## Slide 1
Chart: 
| 0 | 10 | 21.8 | 35 | 45 | 53 | 60 | 78 | 90
Int | 60 | 10 | 25 | 5 | 7 | 2 | 1 | 2 | 1
Wide Angle Scattering (WAXS) (Powder Diffraction)
How do we do
Interaction of X-ray radiation with solids
Data Collection
XRDLab
TAMU
CHEMISTRY
TEXAS A&M UNIVERSITY
Crystalline Semi crystalline Amorphous
Long range order short range order only
“For most crystallographers it is long-range order that sets crystals apart from glasses and amorphous solids. But condensed-matter physicists have recognized that there is a structural continuum between ideal crystals and amorphous solids.” . Gautam Desiraju : Nature 2013
The Solid State
Collision of the X-ray photon with a charged particle causes the component of the particle to oscillate with the same frequency.
The oscillating particle returns to the resting state by emitting a photon that travels outward.
(1)
Where and =
For a diatomic molecule of the same element the 1st maxima (s >0) for Debye’s equation (2nd derivative of 1) will be ~ given
sm then :
K = 1.23
The Math
Debye’s Equation describes the interaction of radiation between two identical “atoms” i and j separated by the distance rij
For a VERY simple system (all orientations are present) where the average contact distances are near 1.5, 2.5 and 5 Å we can predict the scattered pattern given below. (=1.54Å). Intensity decreases (exponentially) as 2 increases
Debye's Equation [ ]describes the
Amorphous WAXS in general terms.
  For a linear ordered system where the same element (atom) is spaced at equal distance(s) of N>2 times then
2
Chart: 
| -2.5132741228718345 | -2.3561944901923448 | -2.1991148575128552 | -2.0420352248333655 | -1.8849555921538759 | -1.7278759594743864 | -1.5707963267948966 | -1.4137166941154069 | -1.2566370614359172 | -1.0995574287564276 | -0.94247779607693793 | -0.78539816339744828 | -0.62831853071795862 | -0.47123889803846897 | -0.31415926535897931 | -0.15707963267948966 | -3.1415926535897933E-3 | 3.1415926535897933E-3 | 0.15707963267948966 | 0.31415926535897931 | 0.47123889803846897 | 0.62831853071795862 | 0.78539816339744828 | 0.94247779607693793 | 1.0995574287564276 | 1.2566370614359172 | 1.4137166941154069 | 1.5707963267948966 | 1.7278759594743864 | 1.8849555921538759 | 2.0420352248333655 | 2.1991148575128552 | 2.3561944901923448 | 2.5132741228718345
N=2 | 2.618 | 2 | 1.382 | 0.82443 | 0.38197 | 0.097887 | 1.501e-32 | 0.097887 | 0.38197 | 0.82443 | 1.382 | 2 | 2.618 | 3.1756 | 3.618 | 3.9021 | 4 | 4 | 3.9021 | 3.618 | 3.1756 | 2.618 | 2 | 1.382 | 0.82443 | 0.38197 | 0.097887 | 1.501e-32 | 0.097887 | 0.38197 | 0.82443 | 1.382 | 2 | 2.618
N=3 | 2.618 | 1 | 0.1459 | 0.030825 | 0.38197 | 0.81381 | 1 | 0.81381 | 0.38197 | 0.030825 | 0.1459 | 1 | 2.618 | 4.7331 | 6.8541 | 8.4223 | 8.9998 | 8.9998 | 8.4223 | 6.8541 | 4.7331 | 2.618 | 1 | 0.1459 | 0.030825 | 0.38197 | 0.81381 | 1 | 0.81381 | 0.38197 | 0.030825 | 0.1459 | 1 | 2.618
N=4 | 1 | 2.7018e-31 | 0.52786 | 1.1393 | 1 | 0.35416 | 6.004e-32 | 0.35416 | 1 | 1.1393 | 0.52786 | 3.002e-32 | 1 | 4.3885 | 9.4721 | 14.118 | 15.9992 | 15.9992 | 14.118 | 9.4721 | 4.3885 | 1 | 3.002e-32 | 0.52786 | 1.1393 | 1 | 0.35416 | 6.004e-32 | 0.35416 | 1 | 1.1393 | 0.52786 | 2.7018e-31 | 1
N=6 | 1 | 2 | 0.52786 | 0.12028 | 1 | 0.67093 | 1.3509e-31 | 0.67093 | 1 | 0.12028 | 0.52786 | 2 | 1 | 0.46331 | 9.4721 | 26.7455 | 35.9959 | 35.9959 | 26.7455 | 9.4721 | 0.46331 | 1 | 2 | 0.52786 | 0.12028 | 1 | 0.67093 | 1.3509e-31 | 0.67093 | 1 | 0.12028 | 0.52786 | 2 | 1
As N increases the peak sharpens until N>1000 atoms at which time you reach the line width of the instrument.
given : then
For a 3D ordered system (Crystalline)
(unit cell as vectors)
Given
and
For the 3D ordered systems will have maxima at discrete positions  2hkl
Source (A)
Specimen (B)
Detector (C)
2
X-rays diverge from the source (A) strike the specimen (B) and converge back to the detector (C) .
h=1,k=1,l=0
h=2,k=1,l=2
I(2,1,2)  F(2,1,2)2 [atoms (e-) in 2,1,2 plane]
Amorphous
Semi crystalline
Crystalline
Zinc Glutamate
Spacegroup P2/c
a (Å) 13.8847(1)
b (Å) 4.7879(3)
c (Å) 9.2663(6)
beta (°) 90.506(3)
Polymorphs
A
B
C
BRAGG BRENTANO :The detector is positioned at 2 angle to collect the data. The number of X-rays counted by the detector is proportional to the intensity (I) of the scattered X-ray
Transmission with Area detection.
The area (2D) detector is positioned behind the sample. X-rays travel; through the sample and are collected at the detector
Fiber Diffraction
Qualitative Analysis
Phase Analysis
Paraffin
1.1.2 2018 TAMU
Structure Determination from Powder Data and Rietveld Refinement
Applications
1.5Å
2.5Å
5Å
2
cum videbimus lumen